## Slide 1
Glycosylated Nanomaterials: Neutralisation and Detection of Bacteria and Toxins
Sarah-Jane Richards &
Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
www.warwick.ac.uk/go/gibsongroup
S-J.Richards@warwick.ac.uk
248th ACS Meeting – 13th August

## Slide 2
Applications: Anti-adhesion Therapy
Interactions can be inhibited at nM of glycopolymers
Sharon, N. Biochimica et Biophysica Acta, 2006, 527–537
Hidari et al. Glycobiology 2008, 18, 779
Influenza inhibition in mice
Notes: Change to cholera
Get rid of HIV

## Slide 3
Glycopolymers by Post-Polymerisation Modification
Jones, M. W., Richards, S-J., Haddleton, D. M. Gibson, M. I.; Polym. Chem., 2013,
Jones, M. W., L. Otten, Richards, S-J., Lowery, R., Phillips, D. J. Haddleton, D. M. Gibson, M. I.; Chem. Sci., 2014
Richards, S-J., Jones, M. W., Hunabun, M. I., Haddleton, D. M., Gibson, M. I.; Angew. Chem., 2012
Notes: Change red pic
Ref at botto,

## Slide 4
Easy to make 50 gram scale
1 column/distillation
Compatible with RAFT/ATRP
Quantitative functionalisation with non-hindered amines
Density control
Sequentially
modified
polymer libraries
Theato, P.; J. Pol. Sci. A., 2008, 46, 6677

## Slide 5
Carbohydrate binding domain
Enzymatic domain
Binds to epithelial cells to promote cell uptake
Induces toxic effect
Selective Binding of Cholera-Toxin
GM-1 ganglioside
β-D Galactose
Galectins – at least 13
Sigma-Aldrich – 8 Galactose-’specific’ lectins
How do we engineer a high-affinity binder for cholera toxin, without total synthesis of complex carbohydrates?
Anti-adhesion therapy does not target bacteria, so less evolutionary stress

## Slide 6
Kiick et al.; Macromol. 2007, 40, 7103 and Biomac., 2006, 7 483
Peanut Agglutinin
Cholera Toxin
Glycan Accessibility as a Tool for Lectin Specificity
6.3 Å
16 Å
Notes: More reference

## Slide 7
Glycopolymer Library
Polymer | DP[a] | Linker[b] | Density[c] | Mw/Mn[d]
GP1 | 18 | Short | 100 | 1.29
GP2 | 33 | Short | 100 | 1.27
GP3 | 70 | Short | 100 | 1.26
GP4 | 18 | Long | 100 | 1.32
GP5 | 33 | Long | 100 | 1.28
GP6 | 70 | Long | 100 | 1.27
GP7 | 33 | Long | 50 | 1.23
GP8 | 33 | Long | 25 | 1.21
GP9 | 33 | Long | 10 | 1.20

## Slide 8
Peanut Agglutinin
Polymer length
Short Linker
Long Linker
Cholera Toxin
Short Linker
Long Linker
Richards, S-J., Jones, M. W., Hunabun, M. I., Haddleton, D. M., Gibson, M. I.; Angew. Chem., 2012, 51, 7812
Polymer length

## Slide 9
Applications: Detection
Direct
Label-free
Easy
Sensitive
Quantifiable in real-time
Notes: More reference

## Slide 10
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
[Con A]
Size dependant aggregation
Con A induced aggregation
Kinetics of colour change
Notes: More reference

## Slide 11
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
TOP10
- FimH
K-12
+ FimH
[FimH+ bacteria]
[FimH- bacteria]
OD = 0.25
OD 0.005
[Bacteria]
Bacteria induced aggregation
Bacteria induced colour change
Colour Change 
Fast 
Specific 
Saline Stability 
Notes: More reference

## Slide 12
Colour change  Specific  Saline Stable 
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
40 nm
n = 68
Bacteria induced aggregation
Con A induced aggregation
PEG functionalised
[ConA]
Directly functionalised
Colour Change 
Fast 
Specific 
Saline Stability
Notes: More reference

## Slide 13
SEC of sizes
Saline stability
Kinetics of colour change
Optimisation of polymer coating
Notes: More reference

## Slide 14
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I., In Preparation
Soy bean agglutinin induced aggregation
Rapid colour change (< 5 mins)
Highly specific change
[SBA]
[SBA]
Aggregation behaviour confirmed by DLS
Colour Change 
Fast 
Specific 
Saline Stability 
Notes: More reference

## Slide 15
Summary
Tandem Post-Polymerisation Modification
Multivalent inhibitors that have good affinity AND specificity
Glycogoldnanoparticles
Optimised polymer coating for lectin detection

## Slide 16
Acknowledgements
Matthew Gibson
Dave Haddleton
Del Besra
Elizabeth Fullam
Mathew Jones
Gibson Group Members
Gemma-Louise Davies - Daniel Mitchell
Yunhua Chen - Richard Lowery
Catherine Cooper - Ben Martyn
Robert Deller - Lewis Blackman
Caroline Biggs - Sang-Ho Won
Daniel Phillips - Laura Wilkins
Tom Congdon - Robert Keogh
Lucienne Otten

## Slide 17
Sarah-Jane Richards & Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
www.warwick.ac.uk/go/gibsongroup
S-J.Richards@warwick.ac.uk
Glycosylated Nanomaterials: Detection and Neutralisation of Bacteria and Toxins
248th ACS Meeting – 13th August

## Slide 18
Underivatised reducing sugars
Lectin Screening and Discrimination
Notes: More reference