## Slide 1
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s.richards.1@warwick.ac.uk
Dr Sarah-Jane Richards and Prof. Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
Brightsparks Symposium 12/09/16
University of Warwick
www.warwick.ac.uk/sarahjane_richards

## Slide 2
Glycans are Crucial Biomarkers
Selection of N-linked mammalian glycans d/load from P Stanley Lab
Cholera
Ricin
Influenza
Ebola
Shiga Toxins
HIV
Non antibiotic solutions to resistance
Treatment
Diagnosis
Understanding

## Slide 3
Label-Free Biosensing

## Slide 4
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
Glycosylated Gold Nanoparticles
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498

## Slide 5
40 nm
n = 68
Con A induced aggregation
PEG functionalised
Directly functionalised
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
PEG-Stabilized AuNPs

## Slide 6
Optimisation of polymer coating
Masked thiol for immobilization on to AuNP
Sugar for lectin recognition
Sugar conjugation site
Thiol for immobilization on to AuNP
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 7
Optimisation of polymer coating
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367
‘Goldilocks’ Particle

## Slide 8
Speed of colour change
Optimisation of Polymer Coating
Saline stability
DP10
DP20
DP75
Colour Change 
Fast 
Specific 
Saline Stability 
Richards, S-J and Gibson, M. I.; Macro Lett., 2014, 2, 1490-1498, 1, 1004-1008
Too short
‘Just right’
Too long

## Slide 9
Polymer coating characterisation
Otten, L., D. Vlachou, Richards, S-J.* Gibson, M. I.; Analyst., 2016, 141, 4305-4312
1:19 ratio
XPS
Notes: Change structure!!

## Slide 10
Soy bean agglutinin induced aggregation
Rapid colour change (< 5 mins)
Highly specific change
[SBA]
[SBA]
Aggregation behaviour confirmed by DLS
Colour Change 
Fast 
Specific 
Saline Stability 
Optimisation Summary
Richards, S-J., Gibson, M. I. ACS Macro Lett.., 2014, 3, 1004-1008

## Slide 11
Toxin 1
Toxin 2
Can ‘never’ have a perfect, single channel glyco-sensor
Improving identification power

## Slide 12
Gal
Man
Otten, L., D. Vlachou, Richards, S-J.* Gibson, M. I.; Analyst., 2016, 141, 4305-4312
Protein identification

## Slide 13
Increasing identification using heterogeneity
Gal
Man
10%
90%
20%
80%
30%
70%
40%
60%
50%
50%
60%
40%
70%
30%
80%
20%
90%
10%
Otten, L., D. Vlachou, Richards, S-J.* Gibson, M. I.; Analyst., 2016, 141, 4305-4312

## Slide 14
Concentration effects on identification
Otten, L., D. Vlachou, Gibson, M. I.; Richards, S-J.* Analyst., 2016, 141, 4305-4312
Gal
Man
10%
90%
20%
80%
30%
70%
40%
60%
50%
50%
60%
40%
70%
30%
80%
20%
90%
10%

## Slide 15
Underivatised reducing sugars
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Towards High-throughput screening

## Slide 16
High-throughput data collection
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2015, DOI: 10.1039/C5TB01994J

## Slide 17
Lectin Screening and Discrimination
Otten, L. O. and Gibson, M. I. RSC Adv., 2015,5, 53911-53914
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Protein identification

## Slide 18
vs
£10,000
£50
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Low cost, low resource detection

## Slide 19
Summary
Polymer coating essential for saline stability and optical readout
Simple protein detection and identification
High-throughput and low resource detection possible

## Slide 20
Undergrad Students
Lizzie Eyre
Josh Parkin
Post-docs
Dr. Sarah-Jane Richards
Dr. Caroline Biggs
Dr Collette Guy
Eva Caamano-Gutierrez
Dr Lucienne Otten
Phd Students
Alaina Emmanuella
Sang Ho Won
Lewis Blackman
Benjamin Martyn
Joseph Healey
Nick Alcaraz
Julia Lipecki
Chris Stubbs
Ben Graham
Trishia Bailey
Laura Wilkins
Maria Gyprioti
Vinko Varas
Gabriell Erni-Cassolla
Acknowledgements
www.warwick.ac.uk/go/gibsongroup
@LabGibson
Funders £$€
Noreen Murray Philanthropy Award

## Slide 21
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s.richards.1@warwick.ac.uk
Dr Sarah-Jane Richards and Prof. Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
Brightsparks Symposium 12/09/16
University of Warwick
www.warwick.ac.uk/sarahjane_richards