## Slide 1
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
250th ACS Meeting 16/08/15
Boston, MA
www.warwick.ac.uk/sarahjane_richards

## Slide 2
Glycans are Crucial Biomarkers
Selection of N-linked mammalian glycans d/load from P Stanley Lab
Cholera
Ricin
Influenza
Ebola
Shiga Toxins
HIV
Non antibiotic solutions to resistance
Treatment
Diagnosis
Understanding

## Slide 3
Label-Free Biosensing

## Slide 4
[ConA]
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
Colour Change 
Fast 
Specific 
Saline Stability 
Glycosylated Gold Nanoparticles

## Slide 5
40 nm
n = 68
Con A induced aggregation
PEG functionalised
Directly functionalised
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
PEG-Stabilized AuNPs

## Slide 6
Optimization of polymer coating
Masked thiol for immobilization on to AuNP
Sugar for lectin recognition
Sugar conjugation site
Thiol for immobilization on to AuNP
Richards, S-J., Biggs, C. I.., Gibson, M. I.; Book Chapter, Accepted

## Slide 7
Conjugation Versatility
Richards, S-J., Biggs, C. I.., Gibson, M. I.; Book Chapter, Accepted

## Slide 8
SEC of sizes
Kinetics of colour change
Richards, S-J and Gibson, M. I.; Macro Lett., 2014, 2, 1490-1498, 1, 1004-1008
Optimization of Polymer Coating
Saline stability

## Slide 9
Soy bean agglutinin induced aggregation
Rapid colour change (< 5 mins)
Highly specific change
[SBA]
[SBA]
Aggregation behaviour confirmed by DLS
Colour Change 
Fast 
Specific 
Saline Stability 
Richards, S-J and Gibson, M. I.; Macro Lett., 2014, 2, 1490-1498, 1, 1004-1008
Lectin Specificity and Speed of Readout

## Slide 10
Underivatised reducing sugars
Richards, S-J., Otten, L. O., Gibson, M. I.; Submitted

## Slide 11
B
A
C
C
Richards, S-J., Otten, L. O., Gibson, M. I.; Submitted
Polymer coating characterisation

## Slide 12
High-throughput data collection
Richards, S-J., Otten, L. O., Gibson, M. I.; Submitted

## Slide 13
Richards, S-J., Otten, L. O., Gibson, M. I.; Submitted
vs
£10,000
£50
Low-Cost, Low-Resource Detection

## Slide 14
Richards, S-J., Otten, L. O., Gibson, M. I.; Submitted
Otten, L. O. and Gibson, M. I. RSC Adv., 2015,5, 53911-53914
Lectin Screening and Discrimination

## Slide 15
Summary
Polymer coating essential for saline stability and optical readout
Vast conjugation space
High-throughput and low resource detection possible

## Slide 16
Treatment
Diagnosis
Understanding
POLY 448: Tandem post-polymerization modification: Routes to effective glycopolymer inhibitors of bacterial toxins.
Grand Ballroom C – Westin Boston Waterfront Hotel
Thursday 10:45 – 11:10

## Slide 17
Dr Matthew Gibson
Prof. Gurdyal Besra
Dr Elizabeth Fullam
Current Gibson Group Members
Dr Gemma-Louise Davies - Daniel Mitchell
Dr Daniel Phillips - Ben Martyn
Dr Tom Congdon - Lewis Blackman
Caroline Biggs - Sang-Ho Won
Lucienne Otten - Laura Wilkins
Acknowledgements

## Slide 18
Glycosylated gold nanoparticle biosensors: Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
250th ACS Meeting 16/08/15
Boston, MA
www.warwick.ac.uk/sarahjane_richards