## Slide 1: Light Scattering: Probing the Effect of Chain Confinement on Thermoresponsive Behaviour
Lewis Blackman
10/12/2014

## Slide 2
Analysis of Polymeric Self-Assemblies
Microscopy
Light Scattering

## Slide 3
Light Scattering
λ
+ Good statistics compared with microscopy (measuring >109 particles at once)
+ Analysis can be conducted in solution with minimal effect on the sample.
Data is fit to a model (multiple structures or completely unknown structures can be very problematic)

## Slide 4
DLS vs SLS
DLS
Fluctuations in intensity with time due to Brownian Motion
SLS

## Slide 5
Dynamic Light Scattering
  Measure changes in scattering intensity over short (e.g. millisecond) timescale
  Changes are related to the speed at which particles move
  This can then be related to the hydrodynamic radius, RH
Stokes-Einstein equation

## Slide 6
Dynamic Light Scattering at Multiple Angles
Measure I(t) at multiple angles (q) and concs (c)
Each measurement gives you a correlation function g2(q,t)
Fit correlation func. to get relaxation time
Single angle measurements do not confirm a spherical morphology, or that sample is under Brownian motion

## Slide 7
Chart: q2/ m-2
| 15290000000000 | 19060000000000 | 23240000000000 | 27810000000000 | 32780000000000 | 38130000000000 | 43860000000000
 | 5.5923e-09 | 5.353e-09 | 6.2225e-09 | 6.6458e-09 | 6.7697e-09 | 7.8342e-09 | 7.825e-09
Static Light Scattering at Multiple Angles
Static light scattering (SLS)
  Measure scattering intensity over long timescales (e.g. 1000τ) and average
Zimm equation
Rayleigh ratio
Optical Constant
Zero q:
Kc/Rθ,0 from intercept
O'Reilly, R. K. Chem. Soc. Rev. 2014, 43, 2412.
- Only valid in the Zimm region (qRg < 1)
Mw from intercept
Rg from gradient

## Slide 8
Static Light Scattering: Zimm Plot Obtains Absolute Values
Cannot be performed if Rg<20 nm
No significant gradient
Zero q, zero c:
A2 from gradient
Mw from intercept
O'Reilly, R. K. Chem. Soc. Rev. 2014, 43, 2412.

## Slide 9
Combining SLS and DLS Data
O'Reilly, R. K. Chem. Soc. Rev. 2014, 43, 2412.

## Slide 10
Complimentary Analysis
Covered in this talk
Light Scattering Techniques
Microscopy
O'Reilly, R. K. Chem. Soc. Rev. 2014, 43, 2412.

## Slide 11
Thermoresponsive Polymers
Cellular Uptake
Controlled Drug Release
Tissue Engineering
Georgiou, T. K. Polymers 2011, 3, 1215.
Okano, T. Biomacromolecules 2009, 10, 1331.
Yang, S. Adv. Mater. 2006, 18, 2905.
Ding, J. Chem. Soc. Rev. 2008, 37, 1473.

## Slide 12
Assessing the Effect of Chain Confinement on Thermoresponsive Behaviour
Increasing hydrophobicity in core
Increasing Nagg but same Rh
Hydrophilic Block
Statistical Hydrophilic/ Hydrophobic Block
O'Reilly, R. K.; Gibson, M. I. Chem. Commun. 2011, 47, 11627.

## Slide 13
Controlling Chain Confinement with Nagg
What is the effect of confinement of chains on thermoresponsive behaviour?
Cloud Point ≠ Cloud Point?
Core is not thermoresponsive:
Corona chains are thermoresponsive:

## Slide 14
Synthesis of Thermoresponsive Amphiphilic Diblock Copolymers
DPNIPAAm | DPnBA | DPDMA | % hydrophobic in core
75 | 40 | 0 | 100%
75 | 36 | 4 | 90%
75 | 32 | 8 | 80%
75 | 28 | 12 | 70%
75 | 20 | 20 | 50%
Chart: MW
100% nBA
Chart: MW
90% nBA
Chart: MW
80% nBA
Chart: MW
70% nBA
Chart: MW
50% nBA

## Slide 15
Chart: percentage nBA in core
| 50 | 80 | 70 | 90 | 100
 | 0.4 | 3.8 | 1.2 | 5.4 | 12.2
Cloud Point Trends
Chart: Temperature/ oC
Chart: Temperature/ oC
Chart: percentage nBA in core
| 50 | 80 | 70 | 90 | 100
 | 31.6 | 34.1 | 32.8 | 36 | 34.4
Hysteresis

## Slide 16
Cloud Point Trends
Low Nagg
Coronal chains free to macroscopically dissolve/precipitate rapidly
High Nagg
Coronal chains sterically hindered so respond slowly to temperature changes
Highly confined chains have to overcome the effects of crowding and entanglement before dissolution is possible
Increasing Temperature
Macroscopic
Aggregation
and Precipitation
Measured
Temperature

## Slide 17
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 21.7781 | 18.1942 | 17.0677 | 16.9639 | 14.8674 | 14.5029 | 13.0749
Probing LCST with light scattering: Corona Stretching
Variable Temperature DLS/SLS at Multiple Angles
Chart: q2/ m-2
| 1750 | 2860 | 4190 | 5710 | 7100
 | 1.2508e+14 | 2.3039e+14 | 3.5014e+14 | 469898086838941 | 5.7521e+14
RH = 18.6 nm
Onset of true thermoresponsive behaviour
Data shown for
90% nBA micelles
Data shown for
90% nBA micelles
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 0.82457 | 0.6269 | 0.55691 | 0.55268 | 0.43037 | 0.39126 | 0.31074

## Slide 18
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 1.0109 | 0.95978 | 0.90663 | 0.63082 | 0.61846 | 0.4884 | 0.3672
Probing LCST with light scattering: Corona Stretching
70% nBA micelles
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 0.86889 | 0.75606 | 0.79794 | 0.51563 | 0.45541 | 0.41481 | 0.31946
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 0.82457 | 0.6269 | 0.55691 | 0.55268 | 0.43037 | 0.39126 | 0.31074
Chart: Temperature/ oC
| 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
 | 0.53582 | 0.51819 | 0.47054 | 0.4221 | 0.32002 | 0.31673 | 0.30708

## Slide 19
Conclusions
Conclusions
Hysteresis of the cloud point in thermoresponsive self-assemblies may be able to be explained by kinetic and steric arguments
The onset of true molecular thermoresponsive behaviour on the nanoscale occurs at much lower temperatures than the cloud point (a macroscopic property)
The rate of corona stretching seems to be independent of Nagg at this chain density

## Slide 20
Acknowledgements
Dan Wright
Dr. Mathew Robin
Dr. Helen Willcock
Prof. Rachel O’Reilly
Dr. Matthew Gibson
O’Reilly and Gibson Groups