## Slide 1
Lewis D. Blackman,* Daniel B. Wright, Mathew P. Robin, Matthew I. Gibson and Rachel K. O’Reilly
University of Warwick, Gibbet Hill Road, Coventry, CV4 7AL, UK
Responsive Assemblies for Biological Applications
@RORgroup @LabGibson

## Slide 2
Thermoresponsive Polymers
Cellular Uptake
Controlled Drug Release
Tissue Engineering
Ward, M. A. Polymers 2011, 3, 1215.
Okano, T. Biomacromolecules 2009, 10, 1331.
Yang, S. Adv. Mater. 2006, 18, 2905.
Ding, J. Chem. Soc. Rev. 2008, 37, 1473.
2

## Slide 3
Thermoresponsive Polymers: pNIPAM
3
pNIPAM
Djokpé, E. Macromol. Chem. Phys. 2001, 202, 750.
Exhibits sharp transition close to body temperature
Insensitive to other environmental conditions
O'Reilly, R. K. Chem. Commun. 2011, 47, 355.
Slow reversibility in certain systems
Heating
Cooling

## Slide 4
Tunable Nagg Micelles
Hydrophilic
Corona-Forming Block
Statistical Hydrophilic/ Responsive Core-Forming Block
4
p(DMAEMA-co-DEAEMA)-b-DMAEMA
O'Reilly, R. K. Polym. Chem. 2015, DOI: 10.1039/C4PY01782J.
What is the effect of Nagg on the thermoresponsive behaviour of a corona block?

## Slide 5
Responsive
Corona-Forming Block
Statistical Hydrophilic/ Hydrophobic Core-Forming Block
5
p(DMA-co-nBA)-b-NIPAM
Diblock Copolymer Design

## Slide 6
Diblock Copolymer Synthesis
6
Polymer | nBA:DMA Feed Ratio | DP nBA | DP DMA | Mol % nBA | Ð
MCTA | N/A | N/A | N/A | N/A | 1.07
1 | 1:1 | 20 | 17 | 54 | 1.10
2 | 7:3 | 26 | 11 | 70 | 1.11
3 | 4:1 | 27 | 7 | 79 | 1.10
4 | 9:1 | 37 | 4 | 90 | 1.11
5 | 1:0 | 40 | N/A | 100 | 1.11

## Slide 7
RH
Micelle Preparation and Characterisation
7
Rcore
Rcorona
Nagg
Multiple angle DLS and SLS

## Slide 8
8
Probing Thermoresponsive Behaviour: Turbidimetry and Microcalorimetry
Two Phase System
Macroscopic Precipitation
Cloud Point
Tp
One Phase System

## Slide 9
9
Probing Thermoresponsive Behaviour: Turbidimetry and Microcalorimetry
Transition temperature does not change with Nagg
Degree of hysteresis increases with increasing nBA composition in core forming block
Tp
Cloud point
Hysteresis

## Slide 10
10
Origin of Hysteresis in Highly Aggregated Micelles
Known to be a kinetic effect
Two Possible Conclusions:
  Differences in intraparticle chain entanglement
  Differences in core hydration
Heated to 40°C
Cooled and held at 30°C

## Slide 11
RH
Probing Thermoresponsive Behaviour: Variable Temperature Light Scattering
Heat
Rcore
Rcorona
Lmax, corona
Coronal Chain Collapse
11

## Slide 12
12
Probing Thermoresponsive Behaviour: Turbidimetry and Microcalorimetry
One Phase System
Coronal Chain Collapse
Two Phase System
Macroscopic Precipitation
Cloud Point
Tp

## Slide 13
The chain collapse and transition temperatures were found to be independent of Nagg
13
Conclusions
Well-defined polymers were synthesised by RAFT polymerisation
The pNIPAM coronal chains were shown to collapse at temperatures lower than the normal transition temperature observed for unimers
The degree of hysteresis was found to increase as a function of Nagg
  Interchain entanglement at high Nagg
  Low rate of water penetration at high nBA content
Coronal Chain Collapse
LLS determined the resultant micelles had tunable Nagg

## Slide 14
14
Acknowledgements
Malvern Instruments Ltd.
Dr. Daniel Wright
Dr. Mathew Robin
Prof. Rachel O’Reilly
Dr. Matthew Gibson
O’Reilly Group
Gibson Group
Funding Sources:
  EPSRC
  BP
  ERC
  IAS
Thank you!
@RORgroup @LabGibson

## Slide 15
Lewis D. Blackman,* Daniel B. Wright, Mathew P. Robin, Matthew I. Gibson and Rachel K. O’Reilly
University of Warwick, Gibbet Hill Road, Coventry, CV4 7AL, UK
Responsive Assemblies for Biological Applications
@RORgroup @LabGibson