## Slide 1
The Effect of Thermoresponsive Micellar Structure on Thermal Hysteresis
www.warwick.ac.uk/gibsongroup
L.D.Blackman@warwick.ac.uk
Lewis D. Blackman, Daniel B. Wright, Mathew P. Robin, Matthew I. Gibson and Rachel K. O’Reilly
Department of Chemistry, University of Warwick, UK
@LabGibson @RORgroup
Macrogroup UK Young Researcher’s Meeting. 06/04/2016
University of Liverpool
www.warwick.ac.uk/ror

## Slide 2
Thermoresponsive Polymers
Cellular Uptake
Controlled Drug Release
Tissue Engineering
Georgiou, T. K. Polymers 2011, 3, 1215. Okano, T. Biomacromolecules 2009, 10, 1331.
Yang, S. Adv. Mater. 2006, 18, 2905. Ding, J. Chem. Soc. Rev. 2008, 37, 1473.
2

## Slide 3
Thermoresponsive Polymers: pNIPAM
pNIPAM
Djokpé, E.; Vogt, W. Macromol. Chem. Phys. 2001, 202, 750.
Exhibits sharp transition close to body temperature
Insensitive to other environmental conditions
Moughton, A. O.; Patterson, J. P.; O'Reilly, R. K. Chem. Commun. 2011, 47, 355.
Slow reversibility in certain systems
Heating
Cooling
3

## Slide 4
Tunable Nagg Micelles
Hydrophilic
Corona-Forming Block
Statistical Hydrophilic/ Responsive Core-Forming Block
p(DMAEMA-co-DEAEMA)-b-DMAEMA
Wright, D. B.; Patterson, J. P.; Pitto-Barry, A.; Cotanda, P.; Chassenieux, C.; Colombani, O.; O'Reilly, R. K. Polym. Chem. 2015, 6, 2761.
What is the effect of Nagg on the thermoresponsive behaviour of a corona block?
4

## Slide 5
Diblock Copolymer Design and Micelle Preparation
Responsive
Corona-Forming Block
Statistical Hydrophilic/ Hydrophobic Core-Forming Block
p(DMA-co-nBA)40-b-NIPAM75
5
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.

## Slide 6
Probing Thermoresponsive Behaviour
Two Phase System
Macroscopic Precipitation
Cloud Point
Tp
One Phase System
6
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.

## Slide 7
Probing Thermoresponsive Behaviour
Transition temperature does not change with Nagg
Degree of hysteresis increases with increasing nBA composition in core forming block
Tp
Cloud point
Hysteresis
7
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.

## Slide 8
Origin of Hysteresis in Highly Aggregated Micelles
Known to be a kinetic effect
Two Possible Conclusions:
  Differences in intraparticle chain entanglement
  Differences in core hydration
Heated to 40 °C
Cooled and held at 30 °C
8
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.

## Slide 9
pNIPAM300
pNIPAM300-b-nBA28
pNIPAM75-b-nBA40
Degree of hysteresis is reduced by increasing weight fraction of the corona
  Differences in core hydration, as opposed to corona entanglement, lead to differences in hysteresis
Origin of Hysteresis in Highly Aggregated Micelles
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.
9

## Slide 10
Investigating Hysteresis Using Other Thermoresponsive Coronas
x = 0.54
x = 0.70
x = 0.79
x = 0.90
x = 1.00
x = 0.50
x = 0.69
x = 0.76
x = 0.88
x = 1.00
x = 0.46
x = 0.68
x = 0.82
x = 0.88
x = 1.00
Polymer
Type
Tg
H bond donor?
6-10
Linear
High
Yes
11-15
Brush-like
Low
No
pDEAm
pNIPAM
pDEGMA
1-5
Linear
High
No
10

## Slide 11
Investigating Hysteresis Using Other Thermoresponsive Coronas
pDEAm
pNIPAM
pDEGMA
11

## Slide 12
pDEAm
pNIPAM
But…
Hysteresis can be introduced by hydrophobic core
Nearly identical corona blocks with almost identical cloud points
Hydrogen bonding ability plays major role in determining hysteresis
Investigating Hysteresis Using Other Thermoresponsive Coronas
12

## Slide 13
Cooling
Heating
pDEGMA
pOEGMA
Similar corona blocks but with different cloud points and side-chain lengths
Corona | mol% nBA | Cloud Point/ °C | Hysteresis/ °C
pDEGMA | 45 | 20.3 | 0.4
pDEGMA | 69 | 21.0 | 0.5
pDEGMA | 77 | 19.8 | 0.1
pDEGMA | 87 | 20.5 | Irreversible
pDEGMA | 100 | 22.1 | Irreversible
Investigating Hysteresis Using Other Thermoresponsive Coronas
13
Cooling
Heating

## Slide 14
Conclusions
14
Blackman, L. D.; Wright, D. B.; Robin, M. P.; Gibson, M. I.; O’Reilly, R. K. ACS Macro Letters 2015, 1210.
Well defined responsive amphiphilic block copolymers were synthesised by RAFT polymerisation.
Multi-angle DLS and SLS revealed the resulting micelles had a tuneable Nagg.
The cloud point transition temperatures were found to be independent of Nagg.
The degree of hysteresis was shown to be dependent on the core block hydrophobicity.
Differences in the hysteresis was a result of differences in micellar core hydration.
Both hydrogen bonding ability and core composition played a role in determining hysteresis.
Coronas with a brush-like architecture showed irreversible phase transitions at high Nagg.
pNIPAM300
pNIPAM300-b-nBA28
pNIPAM75-b-nBA40
pDEAm vs. pNIPAM
pDEGMA
pOEGMA

## Slide 15
Acknowledgements
Malvern Instruments Ltd.
Dr. Daniel Wright
Dr. Mathew Robin
Prof. Rachel O’Reilly
Dr. Matthew Gibson
O’Reilly Group
Gibson Group
15

## Slide 16
The Effect of Thermoresponsive Micellar Structure on Thermal Hysteresis
www.warwick.ac.uk/gibsongroup
L.D.Blackman@warwick.ac.uk
Lewis D. Blackman, Daniel B. Wright, Mathew P. Robin, Matthew I. Gibson and Rachel K. O’Reilly
Department of Chemistry, University of Warwick, UK
@LabGibson @RORgroup
Macrogroup UK Young Researcher’s Meeting. 06/04/2016
University of Liverpool
www.warwick.ac.uk/ror