## Slide 1
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
ICS 2016 18/07/16
New Orleans, LA, USA
www.warwick.ac.uk/sarahjane_richards

## Slide 2
Glycans are Crucial Biomarkers
Selection of N-linked mammalian glycans d/load from P Stanley Lab
Cholera
Ricin
Influenza
Ebola
Shiga Toxins
HIV
Non antibiotic solutions to resistance
Treatment
Diagnosis
Understanding

## Slide 3
Label-Free Biosensing

## Slide 4
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
Glycosylated Gold Nanoparticles
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498

## Slide 5
40 nm
n = 68
Con A induced aggregation
PEG functionalised
Directly functionalised
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
PEG-Stabilized AuNPs

## Slide 6
Optimisation of polymer coating
Masked thiol for immobilization on to AuNP
Sugar for lectin recognition
Sugar conjugation site
Thiol for immobilization on to AuNP
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 7
Conjugation Versatility
S-J. Richards, C. I. Biggs, M. I, Gibson, Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 8
Optimisation of Polymer Coating
Size Exclusion Chromatographs
Kinetics of colour change
Saline stability
Richards, S-J., Gibson, M. I. ACS Macro Lett., 2014, 3, 1004-1008
60 nm

## Slide 9
Soy bean agglutinin induced aggregation
Rapid colour change (< 5 mins)
Highly specific change
[SBA]
[SBA]
Aggregation behaviour confirmed by DLS
Colour Change 
Fast 
Specific 
Saline Stability 
Lectin Specificity and Speed of Readout
Richards, S-J., Gibson, M. I. ACS Macro Lett.., 2014, 3, 1004-1008

## Slide 10
Lectin Discrimination
Otten, L., Vlachou, D, Richards, S-J.*, Gibson, M. I.; Analyst., 2016, 141, 4305-4312
Gal
Man

## Slide 11
Increased Discriminatory Power using Heterogeneity
Gal
Man
10%
90%
20%
80%
30%
70%
40%
60%
50%
50%
60%
40%
70%
30%
80%
20%
90%
10%
Otten, L., Vlachou, D, Richards, S-J.*, Gibson, M. I.; Analyst., 2016, 141, 4305-4312

## Slide 12
Lectin Concentration and Discrimination
Gal
Man
10%
90%
20%
80%
30%
70%
40%
60%
50%
50%
60%
40%
70%
30%
80%
20%
90%
10%
Otten, L., Vlachou, D, Richards, S-J.*, Gibson, M. I.; Analyst., 2016, 141, 4305-4312

## Slide 13
‘In plate’ polymerization
‘In plate’ polymer modification
‘In plate’ AuNP functionalization
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367
Towards High-Throughput Sensing

## Slide 14
High-throughput data collection
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2015, DOI: 10.1039/C5TB01994J

## Slide 15
Otten, L. and Gibson, M. I. RSC Adv., 2015, 5, 53911-53914
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Lectin Discrimination

## Slide 16
vs
£10,000
£50
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Low-cost, Low-resource Detection

## Slide 17
Summary
Polymer coating essential for saline stability and optical readout
Vast conjugation space
High-throughput and low resource detection possible

## Slide 18
Undergrad Students
Lizzie Eyre
Josh Parkin
Post-docs
Dr Caroline Biggs
Dr Collette Guy
Eva Caamano-Gutierrez
Dr Lucienne Otten
PhD Students
Sang Ho Won
Lewis Blackman
Benjamin Martyn
Joseph Healey
Nick Alcaraz
Julia Lipecki
Chris Stubbs
Ben Graham
Trishia Bailey
Laura Wilkins
Maria Gyprioti
Vinko Varas
Gabriell Erni-Cassolla
Acknowledgements
www.warwick.ac.uk/go/gibsongroup
@LabGibson
Funders £$€
Noreen Murray Philanthropy Award
Gibson Group, 2016
Prof. Matthew Gibson
Collaborators
Dr Liz Fuilam
Prof. Del Besra (uni B’ham)

## Slide 19
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
ICS 2016 18/07/16
New Orleans, LA, USA
www.warwick.ac.uk/sarahjane_richards