## Slide 1
Investigating Hysteresis in Thermoresponsive Assemblies
www.warwick.ac.uk/go/gibsongroup
L.D.Blackman@warwick.ac.uk
Lewis D. Blackman, Matthew I. Gibson and Rachel K. O’Reilly
Department of Chemistry, University of Warwick, UK
@LabGibson @RORgroup
RSC Biomaterials Chemistry Meeting. 08/01/2016
University of Birmingham
www2.warwick.ac.uk/fac/sci/chemistry/research/oreilly/oreillygroup/

## Slide 2
Thermoresponsive Polymers
Cellular Uptake
Controlled Drug Release
Tissue Engineering
Georgiou, T. K. Polymers 2011, 3, 1215. Okano, T. Biomacromolecules 2009, 10, 1331.
Yang, S. Adv. Mater. 2006, 18, 2905. Ding, J. Chem. Soc. Rev. 2008, 37, 1473.

## Slide 3
Thermoresponsive Polymers: pNIPAM
pNIPAM
Djokpé, E.; Vogt, W. Macromol. Chem. Phys. 2001, 202, 750.
Exhibits sharp transition close to body temperature
Insensitive to other environmental conditions
Moughton, A. O.; Patterson, J. P.; O'Reilly, R. K. Chem. Commun. 2011, 47, 355.
Slow reversibility in certain systems
Heating
Cooling

## Slide 4
Tunable Nagg Micelles
Hydrophilic
Corona-Forming Block
Statistical Hydrophilic/ Responsive Core-Forming Block
p(DMAEMA-co-DEAEMA)-b-DMAEMA
Wright, D. B.; Patterson, J. P.; Pitto-Barry, A.; Cotanda, P.; Chassenieux, C.; Colombani, O.; O'Reilly, R. K. Polym. Chem. 2015, 6, 2761.
What is the effect of Nagg on the thermoresponsive behaviour of a corona block?

## Slide 5
Diblock Copolymer Design and Micelle Preparation
Responsive
Corona-Forming Block
Statistical Hydrophilic/ Hydrophobic Core-Forming Block
p(DMA-co-nBA)40-b-NIPAM75

## Slide 6
Probing Thermoresponsive Behaviour
Two Phase System
Macroscopic Precipitation
Cloud Point
Tp
One Phase System

## Slide 7
Probing Thermoresponsive Behaviour
Transition temperature does not change with Nagg
Degree of hysteresis increases with increasing nBA composition in core forming block
Tp
Cloud point
Hysteresis

## Slide 8
Origin of Hysteresis in Highly Aggregated Micelles
Known to be a kinetic effect
Two Possible Conclusions:
  Differences in intraparticle chain entanglement
  Differences in core hydration
Heated to 40°C
Cooled and held at 30°C

## Slide 9
Investigating Hysteresis Using Other Thermoresponsive Coronas
x = 0.54
x = 0.70
x = 0.79
x = 0.90
x = 1.00
x = 0.50
x = 0.69
x = 0.76
x = 0.88
x = 1.00
x = 0.46
x = 0.68
x = 0.82
x = 0.88
x = 1.00
x = 0.50
x = 0.70
x = 0.80
x = 0.90
x = 1.00
Polymer
Type
Tg
H bond donor?
6-10
Linear
High
Yes
11-15
Brush-like (short side arm)
Low
No
15-20
Brush-like (long side arm)
Low
No
pDEAm
pNIPAM
pDEGMA
pOEGMA
1-5
Linear
High
No

## Slide 10
pDEAm
pNIPAM
But…
Hysteresis can be introduced by hydrophobic core
Nearly identical corona blocks with almost identical cloud points
Hydrogen bonding ability plays major role in determining hysteresis
Investigating Hysteresis Using Other Thermoresponsive Coronas

## Slide 11
pDEGMA
pOEGMA
Similar corona blocks but with different cloud points and side-chain lengths
Corona | mol% nBA | Cloud Point/ °C | Hysteresis/ °C
pDEGMA | 45 | 20.3 | 0.4
pDEGMA | 69 | 21.0 | 0.5
pDEGMA | 77 | 19.8 | 0.1
pDEGMA | 87 | 20.5 | Irreversible
pDEGMA | 100 | 22.1 | Irreversible
pOEGMA | 50 | ~72 | ?
pOEGMA | 70 | ~72 | ?
pOEGMA | 80 | ~72 | ?
pOEGMA | 90 | ~72 | ?
pOEGMA | 100 | ~72 | ?
Investigating Hysteresis Using Other Thermoresponsive Coronas

## Slide 12
Conclusions
The degree of hysteresis increased as a function of core hydrophobicity.
Well-defined polymers were synthesised by RAFT polymerisation.
The transition temperatures were found to be independent of Nagg or core hydrophobicity.
The hydrogen bonding character of the corona played a role in determining the reversibility of the transition.
LLS determined the resultant micelles had tunable Nagg by tuning the core composition.
Brush-like pDEGMA coronas with highly hydrophobic cores showed irreversible phase behaviour
Interchain entanglement?
Moderate hydrophilicity of pDEGMA?

## Slide 13
Acknowledgements
Malvern Instruments Ltd.
Dr. Daniel Wright
Dr. Mathew Robin
Prof. Rachel O’Reilly
Dr. Matthew Gibson
O’Reilly Group
Gibson Group

## Slide 14
Investigating Hysteresis in Thermoresponsive Assemblies
www.warwick.ac.uk/go/gibsongroup
L.D.Blackman@warwick.ac.uk
Lewis D. Blackman, Matthew I. Gibson and Rachel K. O’Reilly
Department of Chemistry, University of Warwick, UK
@LabGibson @RORgroup
RSC Biomaterials Chemistry Meeting. 08/01/2016
University of Birmingham
www2.warwick.ac.uk/fac/sci/chemistry/research/oreilly/oreillygroup/

## Slide 15
pNIPAM300
pNIPAM300-b-nBA28
pNIPAM75-b-nBA40
Degree of hysteresis is reduced by increasing weight fraction of the corona
  Differences in core hydration, as opposed to corona entanglement, lead to differences in hysteresis
Origin of Hysteresis in Highly Aggregated Micelles

## Slide 16
Coronal Chain Collapse in the Single Phase Region
RH
Heat
Rcore
Rcorona
Lmax, corona
Coronal Chain Collapse