## Slide 1
Glycosylated gold nanoparticle biosensors
s.richards.1@warwick.ac.uk
Dr Sarah-Jane Richards and Prof. Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
NanoSymposium 13/12/16
University of Birmingham
www.warwick.ac.uk/sarahjane_richards

## Slide 2
Glycans are Crucial Biomarkers
Selection of N-linked mammalian glycans d/load from P Stanley Lab
Cholera
Ricin
Influenza
Ebola
Shiga Toxins
HIV
Treatment
Diagnosis
Understanding

## Slide 3
Label-Free Biosensing

## Slide 4
[Con A]
Glycosylated Gold Nanoparticles
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
Colour Change 
Fast 
Specific 
Saline Stability 

## Slide 5
40 nm
n = 68
Con A induced aggregation
PEG functionalised
Directly functionalised
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498
[ConA]
Colour Change 
Fast 
Specific 
Saline Stability 
PEG-Stabilised AuNPs

## Slide 6
Optimisation of polymer coating
Masked thiol for immobilisation on to AuNP
Sugar for lectin recognition
Sugar conjugation site
Thiol for immobilisation on to AuNP
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 7
Speed of colour change
Saline stability
DP10
DP20
DP75
Colour Change 
Fast 
Specific 
Saline Stability 
Richards, S-J and Gibson, M. I.; Macro Lett., 2014, 2, 1490-1498, 1, 1004-1008
Too short
‘Just right’
Too long
Finding the ‘Goldilocks’ Zone for Optimised Responses

## Slide 8
Demonstration of Improved Performance
[SBA]
[SBA]
Dynamic Light Scattering
Specificity test
UV-Vis Titration
Kinetics
Richards, S-J., Gibson, M. I. ACS Macro Lett.., 2014, 3, 1004-1008

## Slide 9
Towards a ‘Real’ Colourimetric Sensor
Enzymatic domain
Carbohydrate binding domain
Cholera Toxin
Ricin
3-5 million cases a year
100-120,000 deaths
~1.8 mg to kill 1 person
Vomiting
Diarrhea
Dehydration
Drop in blood pressure
Clinical shock
Vomiting
Diarrhea
Dehydration
Drop in blood pressure
Clinical shock
Stomach cramps
Death
Seizures
Hematuria
Multiple organ failure
Death

## Slide 10
Cholera
Ricin
Can ‘never’ have a perfect, single channel glyco-sensor
Single vs Multi Channel Sensors

## Slide 11
Combinatorial Glyco-AuNP Polymer Libraries
N2H4
Reducing sugar capture
Transmission Electron Microscopy
Dynamic Light Scattering
X-Ray Photo-electron Spectroscopy

## Slide 12
Combinatorial Glyco-AuNP Polymer Libraries
Plate-Reader
1
3
2
4
UV-Vis Traces
1
3
2
4
Dose-response curve
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053

## Slide 13
Decoding the Barcode to Identify Toxins
6 channels to distinguish between 6 lectin inputs
Linear Discriminant Analysis
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Notes: Second is bacteria identification

## Slide 14
Low Cost Approach using a Mobile Phone?
Red/Blue Channel separation
Comparison verses UV/Vis
Mobile Phone Image
Richards, S-J., Otten, L., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053

## Slide 15
Masters Students
Nick Vail
Peiwen Seng
Post-docs
Dr Caroline Biggs
Dr Collette Guy
Dr Lucienne Otten
Dr Muhammad Hasan
Dr Kathryn Styles
PhD Students
Sang Ho Won
Lewis Blackman
Benjamin Martyn
Joseph Healey
Nick Alcaraz
Julia Lipecki
Chris Stubbs
Ben Graham
Trisha Bailey
Laura Wilkins
Maria Gyprioti
Vinko Varas
Gabriell Erni-Cassolla
Robyn Wright
Iain Galpin
Acknowledgements
www.warwick.ac.uk/go/gibsongroup
@LabGibson
Noreen Murray Philanthropy Award

## Slide 16
Glycosylated gold nanoparticle biosensors
s.richards.1@warwick.ac.uk
Dr Sarah-Jane Richards and Prof. Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
NanoSymposium 13/12/16
University of Birmingham
www.warwick.ac.uk/sarahjane_richards

## Slide 17
One more thing… Measurement in (‘real’) Complex Media
‘Binding’ AuNP
‘Non-binding’AuNP
Background removal
Positive
Negative
Unpublished results