## Slide 1
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
Warwick Polymers 2016
Warwick, UK 14/07/16
www.warwick.ac.uk/sarahjane_richards

## Slide 2
Glycans are Crucial Biomarkers
Selection of N-linked mammalian glycans d/load from P Stanley Lab
Cholera
Ricin
Influenza
Ebola
Shiga Toxins
HIV
Non antibiotic solutions to resistance
Treatment
Diagnosis
Understanding

## Slide 3
Label-Free Biosensing

## Slide 4
[Con A]
Colour Change 
Fast 
Specific 
Saline Stability 
Glycosylated Gold Nanoparticles
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498

## Slide 5
40 nm
n = 68
Con A induced aggregation
PEG functionalised
Directly functionalised
[Con A]
Colour Change 
Fast 
Specific 
Saline Stability 
PEG-Stabilized AuNPs
Richards, S-J., Fullam, E., Besra, G. S. Gibson, M. I.; J. Mater. Chem. B, 2014, 2, 1490-1498

## Slide 6
Optimisation of polymer coating
Masked thiol for immobilization on to AuNP
Sugar for lectin recognition
Sugar conjugation site
Thiol for immobilization on to AuNP
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 7
Conjugation Versatility
S-J. Richards, C. I. Biggs, M. I, Gibson, Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367
Richards, S-J., Biggs, C. I, Gibson, M. I., Methods in Molecular Biology; Macro-Glycoligands, 2016, Series Vol 1367

## Slide 8
Optimisation of Polymer Coating
Size Exclusion Chromatographs
Kinetics of colour change
Saline stability
Richards, S-J., Gibson, M. I. ACS Macro Lett., 2014, 3, 1004-1008
60 nm

## Slide 9
Polymer coating characterisation
Otten, L., D. Vlachou, Richards, S-J.*, M.I. Gibson, Analyst., 2016, 141, 4305-4312
Notes: Change structure!!

## Slide 10
Polymer coating characterisation
PVP
POEGMA
Ieong, N.S, Biggs, C.I., Walker, M., Gibson, M.I., In Preparation

## Slide 11
Soy bean agglutinin induced aggregation
Rapid colour change (< 5 mins)
Highly specific change
[SBA]
[SBA]
Aggregation behaviour confirmed by DLS
Colour Change 
Fast 
Specific 
Saline Stability 
Lectin Specificity and Speed of Readout
Richards, S-J., Gibson, M. I. ACS Macro Lett., 2014, 3, 1004-1008

## Slide 12
Underivatised reducing sugars
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053
Towards High-throughput sensing

## Slide 13
High-throughput data collection
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053

## Slide 14
Otten, L. O. and Gibson, M. I. RSC Adv., 2015,5, 53911-53914
Lectin Screening and Discrimination
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053

## Slide 15
vs
£10,000
£50
Low-Cost, Low-Resource Detection
Richards, S-J., Otten, L. O., Gibson, M. I.; J. Mater Chem. B., 2016, 4, 3046-3053

## Slide 16
Summary
Polymer coating essential for saline stability and optical readout
Vast conjugation space
High-throughput and low resource detection possible

## Slide 17
Undergrad Students
Lizzie Eyre
Josh Parkin
Post-docs
Dr Caroline Biggs
Dr Collette Guy
Eva Caamano-Gutierrez
Dr Lucienne Otten
PhD Students
Sang Ho Won
Lewis Blackman
Benjamin Martyn
Joseph Healey
Nick Alcaraz
Julia Lipecki
Chris Stubbs
Ben Graham
Trishia Bailey
Laura Wilkins
Maria Gyprioti
Vinko Varas
Gabriell Erni-Cassolla
Acknowledgements
www.warwick.ac.uk/go/gibsongroup
@LabGibson
Funders £$€
Noreen Murray Philanthropy Award
Gibson Group, 2016
Prof. Matthew Gibson
Collaborators
Dr Liz Fuilam
Prof. Del Besra (uni B’ham)

## Slide 18
Glycosylated gold nanoparticle biosensors:
Label-free and high-throughput evaluation of glycan-lectin interactions
s-j.richards@warwick.ac.uk
Sarah-Jane Richards and Matthew I. Gibson
Department of Chemistry, University of Warwick, UK
@LabGibson
@RichardsSJ
Warwick Polymers 2016 14/07/16
Warwick, UK
www.warwick.ac.uk/sarahjane_richards