## Slide 1
Background References
Acknowledgements
Glycosylated nanomaterials: Detection of pathogenic bacteria and toxins
Sarah-Jane Richards, Elizabeth Fullam, Gurdyal Besra and Matthew I. Gibson
S-J.Richards@warwick.ac.uk
www2.warwick.ac.uk/go/gibsongroup
Richards, S-J.; Fullam, L. C.; Besra, G. S.; Gibson M. I., J. Mater. Chem., 2014
Incorrect glycan = no interaction
Correct glycan = interaction
Colour change  Specific 
Fast  Saline Stable 
Richards, S-J.; and Gibson M. I., ACS Macro Lett., 2014
Size dependant aggregation
Lectin (Con A) induced aggregation
Kinetics of colour change
Synthesis of Directly glycosylated
Size dependant kinetics of colour change
The identiﬁcation of bacterial infections remains a major healthcare challenge, especially to ensure appropriate application of a limited spectrum of antibiotics.
Protein-carbohydrate interactions mediate a multitude of biological processes.
The proteins responsible for these interactions are termed lectins
Goldnanoparticles (AuNPs) have interesting optical properties. Red in solution  blue upon aggregation.
Glycosylated AuNPs (glycoAuNPs) could be used to detect bacteria and lectins.
TOP10
- FimH
K-12
+ FimH
[FimH+ bacteria]
OD 0.25
OD 0.005
[Bacteria]
Bacteria induced aggregation
Bacteria induced colour change
Colour Change 
Fast 
Specific 
Saline Stability 
RAFT derived glycopolymers
DP15, 20, 25, 50 and 75
DP 10 and 15 not saline stable
Optimised for saline stability and speed of readout
Lectin Selectivity
Highly lectin specific
Gal particles aggregate at low SBA concentration whereas Man particles do not
@RichardsSJ
@LabGibson
Ultra-fast kinetics
C. R. Bertozzi, L. L. Kiessling, Science, 2001, 291, 2357
M. Ambrosi, N. R. Cameron, B. G. Davis, Org. Biomol. Chem., 2005, 3, 1593
C. C. Lin, Y. C. Chen, C. Y. Yang, G. F. Chen, Y. C. Chen, Y. C. Wu, C. C. Chen, Chem, Commun, 2003, 2920.
Dr Matthew Gibson
Gibson Group
Prof. Gurdyal Besra (B’ham)
Dr Elizabeth Fullam