## Slide 1
Biomimetic microsystem for the generation and detection of ratiometrically encoded semiochemicals
Z. Racz, M. Cole. J.W. Gardner, S. Pathak
University of Warwick, United Kingdom
H. Gardeniers, W. Bula, N. Dimov
MESA+ Institute for Nanotechnology, Netherlands
D. Markovic, J. Challiss
University of Leicester, United Kingdom

## Slide 2
Fundamentals of Surface Acoustic Waves
Chemoemission
    Atomization by acoustic waves
    Emission by micromachined device
    Wind tunnel results
Chemodetection
    Detection by quartz crystal microbalance
    Detection by SAW device
Outlook and applications
Contents

## Slide 3
Fundamentals of Surface Acoustic Waves
Gold electrode
IDT spacing
Piezoelectric substrate
Piezoelectric and reverse piezoelectric effect
Electric potential is generated in response to mechanical stress
Mechanical deformation occurs when electric field is applied
Surface acoustic wave generation using periodic electrodes
Periodic alternating potential creates acoustic surface wave

## Slide 4
Pheromone container
Particle emission with piezoelectric-atomizer
3 mm
Piezoelectric aerosol nozzle
Control circuit
Notes: Advantage: frequency can be modified
Disadvantage: wetting properties must be properly designed

## Slide 5
f [Hz] | 50k | 100k | 500k | 1M | 3M | 5M | 10M
d [µm] | 22.5 | 14.2 | 4.8 | 3.0 | 1.5 | 1.0 | 0.7
Chart: Atomizer frequency [MHz]
| 50000 | 100000 | 500000 | 1000000 | 3000000 | 5000000 | 10000000
Water | 22.4691 | 14.1546 | 4.8408 | 3.0495 | 1.4661 | 1.0429 | 0.657
Estimated droplet diameter for water:
Control of odorant droplet size
Droplet size can be controlled by frequency but wetting properties must be designed carefully

## Slide 6
Ni/Co membranes on piezoelectric atomizers
USB data acquisition unit
141 kHz square wave generator
CMOS analog switch
Microcontroller
LabVIEW interface

## Slide 7
M. Alvarez et. al. Nanotechnology 19 (2008)
K. Chono et. al. IEEE Ultrasonics Symposium (2003)
Atomization by Surface Acoustic Waves
Provides three modes of particle generation but frequency is fixed
Notes: Advantage: Three modes of particle generation
Disadvantage: Frequency is fixed

## Slide 8
Micromachined device for ligand emission: Artificial gland
Evaporation drives emission
Rate of emission controlled by surface morphology and temperature
Cuticular hairs of Helicoverpa zea, showing droplets of extraction
(Raina et al., 2000)
Porous silicon
Black silicon

## Slide 9
Second generation of Artificial gland for integration with biosynthetic microreactor
heaters
membrane
membrane has tuned wettability
biomimic: black silicon surface
to micro reactor

## Slide 10
Chip size:
20 mm x 15 mm
Artificial gland – fabrication results

## Slide 11: Ligand selection: Fruit volatiles and pheromones
Chemical | GC (%)
butyl hexanoate | 37
pentyl hexanoate | 5
propyl hexanoate | 4
butyl butanoate | 10
hexyl butanoate | 44
butyl hexanoate | 0.01
3-methylbutan-1-ol | 4
isoamyl acetate | 1.5
4,8-dimethyl-1,3(E),7-nonatriene | 0.09
ethyl acetate | 94.3
dihydro--ionone | 0.10
-caryophyllene | 5.8
3-methylbutan-1-ol | 27.5
isoamyl acetate | 0.9
1-octen-3-ol | 9
ethyl acetate | 54.9
dimethyl trisulfide | 1.9
Apple
Hawthorn
Dogwood
(Linn et. al, 2005)

## Slide 12: Ligand transfer – Volatile fluid dynamics
Wind tunnel experiments for evaporation rates and detection limits (Dr. Carot)
Mini-scale wind tunnel: odour chamber
Sensor array
Computer interface
Inlet ports
Odour chamber

## Slide 13: Detection: Quartz crystal microbalances (QCMs)
Frequency shift due to mass change:
Sensitivity: ∆f = 7.2 Hz/ng
AC
Gold electrode
Quartz crystal
Gas sensitive coating
Gold electrode
3 mm
Sauerbrey equation

## Slide 14: Ligand detection using QCMs
 | Odorant | PSF | PSB | PEG | PMMA
1. seq. | 3m | 137 | 144 | 110 | 42
 | HB | 127 | 103 | 58 | 29
 | EA | 136 | 57 | 35 | 28
 | BH | 134 | 87 | 33 | 32
2. seq. | BH | 59 | 77 | 26 | 15
 | HB | 98 | 127 | 31 | 14
 | EA | 157 | 28 | 59 | 26
 | 3m | 90 | 39 | 46 | 18
3. seq. | 3m | 80 | 39 | 49 | 16
 | HB | 82 | 138 | 57 | 24
 | BH | 69 | 118 | 53 | 22
 | EA | 130 | 33 | 31 | 22
-4
-2
0
2
4
6
DF1: 40.3%
-4
-2
0
2
4
DF2: 30.9%
3m
EA
BH
HB

## Slide 15: Blend Coding for Fruit Components
1:1
1:3
3:1
Plots showing the concept of ratiometric coding using two chemical components (a) and the target results of such an experiment (b).

## Slide 16: Output from first prototype system
Frequency change of PCL coated QCM vs. Frequency change of PSB coated QCM in response to a randomized sequence of 36 injections of an ethyl acetate/3-methylbutan-1-ol mixture of varying concentration and mixing ratio

## Slide 17: Detection II: SAW Delay Line Device
a)
b)
Output IDT
Input IDT
Launched surface wave
Sensing area
Piezoelectric substrate
Very sensitive to mechanical and electrical perturbations
Simple, robust design
Uniform sensing area
Large sensing area
Output: attenuation and phase
Similar principle of operation as QCMs:

## Slide 18: Principle of SAW bio-probe
 | Thickness [nm] | Frequency [MHz] | Feature size [nm]
Poly-D-lysine | 15 | 39,901 | 26
Bilipid layer | 22.5 | 26,600 | 39
Edge of cell | 615 | 973 | 1,069
Middle of cell | 7,515 | 80 | 13,064
Upright cell | 15,015 | 40 | 26,102
PDL
Bilipid layer
Cell edge
Nucleus
LiTaO3 substrate
www.bio.miami.edu
www.unm.edu
ardb.bjmu.edu.cn
25 MHz SAW
penetrates yeast cells
5 GHz SAW penetrates
10 nm coating
GHz for GPCR or antibodies

## Slide 19: Dual SAW biosensor output
Cell + OR22a + ligand
Cell + ligand
FREE DUAL SAWs
SHORTED DUAL SAWs
-
=
SAW sensor
SAW sensor

## Slide 20: Simplified Artificial Antennal Lobe!
Interface circuitry
Cell + OR67d + ligand
Cell + ligand
-
Cell + OR83b + ligand
Cell + ligand
-
SAW sensor
SAW sensor
SAW sensor
SAW sensor
Cell + OR22a + ligand
Cell + ligand
-
SAW sensor
SAW sensor
FPGA with neuromorphic model

## Slide 21
HEK cell coated SAW sensors
Cell deposition
SAW device
Liquid chamber
20 μm
2.5 μm
HEK cells on SAW device
HEK cells on SAW device

## Slide 22
Biosensor characterization setup
Optical Microscope
Network Analyser
SAW Sensor with HEK293 cells
Real time cell monitoring
Dry-Block Heater for Temperature Control
Notes: Main advantages of the measurement setup
provides temperature control
allow simultaneous optical microscopic and electrical characterization
enables continuous measurement and monitoring
allows characterization without disturbing or stressing the cells

## Slide 23: Prototype Infochemical System
Gland
interface
Emitter
Pump
Receiver
QCM interface

## Slide 24: Summary
Piezoelectric chemoemitter and micro-evaporator presented
Cell based piezoelectric chemodetector with insect ORs designed
Prototype infochemical system shown
Ratiometrically encoded food volatiles discussed
Pheromone bioreactor under construction

## Slide 25: Outlook
Integrate artificial gland and biosensors into CMOS compatible microsystem
Real world applications:
    platform to explore semiochemistry)
    insect semiochemistry (interference with insect communication, crop protection)

## Slide 26: Acknowledgements
Financial support from EU FP6 FET programme – iCHEM project
See: www.warwick.ac.uk/go/iCHEM