## Slide 1: Predictive modelling: a view from the atomic level
P.M. Rodger
Department of Chemistry
& Centre for Scientific Computing
University of Warwick

## Slide 2: Acknowledgements
David Quigley, Igor Khovanov, Matt Bano, Yuriy Bushuev, Aaron Finney, Ritchie-Mae Gamot, Yuanwei Xu, Salvatore Cosseddu (Warwick)
John Harding, Colin Freeman and Riccardo Innocenti Malini (Sheffield)
Paul Smeets, Heiner Friedrich, Jozua Laven, Nico Sommerdijk (Eindhoven), Wouter Habraken (Postdam), Fabio Nudelman (Edinburgh)
Mike Allen (Warwick), Dorothy Duffy (UCL), Julian Gale (Curtin)
Warwick CSC
HECToR & ARCHER
MidPlus
EPSRC (mIb: Materials Interfacing Biology)

## Slide 3: Philosophy
Complex materials
  complete model is not possible
Mechanistic information
  “predictions” not reliable without the correct underlying physics/chemistry
Dimensionality
  identify key degrees of freedom
  target analysis
  drive or simplify modelling

## Slide 4: Unexpected Mechanisms: old examples

## Slide 5: Motivation: Biominerals
Nature:
  Exquisite control of crystal morphology & aggregation found in nature
  Leads to very well “designed” functional materials
  Ability to simulate implies ability to guide synthesis
Henriksen, K., S. L. S. Stipp, et al. American Mineralogist 89, 1709-1716 (2004)
Emiliania huxleyi coccoliths
Reddy, M. M. and A. R. Hoch. Journal of Colloid and Interface Science 235, 365-370 (2001)
Laboratory:

## Slide 6: Motivation: additives for inhibition
Often need to suppress crystal growth
  Scale, wax, hydrate
“kinetic” inhibitors
  Delay nucleation or slow growth
  Active at low concentrations
  Require molecular understanding of nucleation and growth

## Slide 7: Mechanistically inspired prediction?
Inhibition by surface adsorption
validate
screen
new modes?

## Slide 8: Synthesise and test
THF Hydrate Tests
induction times for 0.5% mixtures of tba3S (the “quat”, or Q) and PVP (P). The Control contains no inhibitor. Bars indicate  one standard deviation
Ethane Hydrate Tests
Induction times, nucleation rates (Rnucl) and growth rates (Rgrowth). Standard deviations are given in parentheses

## Slide 9: 2nd generation
2nd generation inhibitors perform about 4 times better than current commercial inhibitor
Test
KI
Gas
Test P/T
Subcooling
Induction
No.
psia/C
/C
Time/ hrs
1
JI-C003:1
NG
1023 / 5.3
10.7
5
2
JI-C003:1
NG
1023 / 5.3
10.7
>67
3
JI-C003:1
NG
1015 / 5
11
>67
4
JI-C003:1
NG
1023 / 5
11
>150
Commercial
NG
10
16
6
JI-C002:1
NG
1095 / 4.5
12.3
3
7
JI-C002:1
NG
1095 / 4
12.8
40
8
JI-C002:1
NG
1095 / 5
11.8
>42
Commercial
5
JI-C003:1
Methane
1700 / 4.5
10
>150
Methane
10
5

## Slide 10: But!
Experiments not repeatable!
  Oil companies can’t repeat each other’s screens
  Heriot-Watt: activity changed with test-cell stirrer design
  Scale of activity with new compound by test-site
    Heriot-Watt > Toulouse > Halliburton > Heriot-Watt
Similar story with wax inhibition (model oil using well characterised edible oil mixture)
Experimentalists working with nanotoxicology want legislative standards based on computational tests because experiments are too irreproducible!
Simplistic model: dynamic interface; nucleation; …

## Slide 11: Nucleation from MD?
Homogeneous nucleation?
  Experimental nucleation rates < O(106) nuclei per cm3 per second
  MD simulation 10,000 molecules:
    1 nucleation event every 32 millenia!
Heterogeneous nucleation?
  (some) success with seeding
  (some) success with interfaces

## Slide 12: Standard MD: modelling surfaces
Deposition of wax on Fe2O3
  C28 from C7

## Slide 13: Standard MD: crystal nucleation
heterogeneous and/or high supersaturation/subcooling

## Slide 14: Polydispersity in inhibitors
molecular weight
  amount of hydrate present
  PVP
molecular shape
  growth of hydrate clusters
  pDMAEMA

## Slide 15: Nucleation more generally
Project onto “important” manifold
  Define key dimensions (order parameters / reaction coordinates / collective variables)
  Project analysis onto these dimensions
  Bias simulations to explore these dimensions
    constrain to portion of manifold (umbrella sampling)
    trap fluctuations that explore the manifold (adaptive bias force)
    disfavour current portion of manifold (Wang-Landau; metadynamics)

## Slide 16:  Free energy hypersurfaces
peptide folding
Bussi, …, Parrinello
3-basin model
Quigley, PMR
KcsN ion channel
Cosseddu, PMR, Khovanov

## Slide 17: Limitations and Pitfalls: dimensionality!
Equilibrium / comprehensive sampling
  Typically 1–2D (≤ 6; can do ~100 for basin escape & rough sampling)
  projection merges basins
Adiabatic Surfaces
  dynamics defined by metastable substates?
KcsN
Potential of mean force
Kramers potential

## Slide 18: Nucleation with metadynamics: ice
4D bias:
  Q4, Q6, ς and potential energy (simaltaneous)
NPT simulation
  density change is spontaneous
T = 180 K; ca. 11 “ns” simulation
Results independent of periodic boundaries

## Slide 19: An ensemble of critical nuclei
N = 147
N = 138
N = 157
N = 161
ice Ic
ice Ih
both

## Slide 20: Nucleation with metadynamics: CaCO3
6 order parameters
  Q4 for: Ca-Ca, Ca-C, Ca-O, C-C, C-O
    measures orientations of X about Y
  energy associated with CaCO3
ca. 10 ns of MD
Exploring configurations
for 75 units (water not shown)

## Slide 21: Calcium Carbonate Biominerals
Multi-stage hierarchical formation
organic “control”
Colfen & Mann Angew. Chem, 2003

## Slide 22: Early stages of carbonate biomineralisation
ions & ion pairs  hACC  ACC  crystalline
hACC: hydrated amorphous calcium cabonate composition ca. CaCO3.H2O
ACC: (anhydrous) amorphous calcium carbonate
Crystalline: calcite, aragonite, vaterite
ions & ion pairs  hACC  ACC  crystalline

## Slide 23: Free energy maps: 75 CaCO3 units
NVT
favours amorphous
DQ and PMR, J. Chem. Phys. 128 (2008) 221101

## Slide 24: Free energy maps: 75 CaCO3 units
NPT
Dominated by calcite
  very low barrier (10–20 kT)
DQ, CLF, JHH and PMR, J. Chem. Phys. 134 (2011) 044703

## Slide 25: 300 CaCO3 Units in water
two stable states
calcite (dominant)
amorphous
energy barrier > 102 kT
multiple transitions

## Slide 26: Biomineralisation: egg shells

## Slide 27: Structure of an eggshell

## Slide 28: G-type lectin-type proteins
found in
  Rhea
  Duck
  Chicken
  Emu
  Ostrich

## Slide 29: Ovocleidin-17
Reyes-Grajeda, Moreno, Romero;
J. Biol. Chem., 2004

## Slide 30: metaDynamics of OC17 + CaCO3
192 & 300 unit nanoparticles
  22,000 water molecules
20 different protein/nanoparticle orientations
Select “best” 4 for long meta-dynamics
Potentials: due to Freeman et al.
  Pavese CaCO3 ; Amber protein; Tip3p water;
  cross terms derived from crystals with scaled charges

## Slide 31: Free energy landscapes
192 units of CaCO3 in water
Initial
metadynamics
Crystallised
192 units of CaCO3 bound to Ovocleidin-17 in water

## Slide 32: Larger nonaparticles?
300 CaCO3 unit particles don’t stay bound on crystallisation
Mechanism for proteins
  Bind to small nanoparticles
  Facilitate transformation to calcite
  Desorb as crystal grows
Gives catalytic cycle for polycrystalline mamillary layer

## Slide 33: OC17: catalytic cycle?
Cryst.
grow
desorb
adsorb

## Slide 34: Surface binding & structured water
Binding is seen to planar surfaces
  Structured water dominates adsorption energy on large crystalline surfaces
  Calcite nanoparticles and ACC do not give structured water layer; leads to “flat” adsorption

## Slide 35: Also seen with AuBP1 on gold
(100) 5x1
(100)
(111)

## Slide 36: hACC nulcleation
Problem
  intermolecular potentials
Controversy

## Slide 37: Aragonite?
needs a better potential (Gale & co workers)
Pavese, Catti, Parker, Wall, Phys Chem. Miner. , 1996
Raiteri, Gale, Quigley, Rodger, J. Phys. Chem. C, 2010

## Slide 38: Structure of hACC
create with several protocols
  melt monohydrocalcite; melt and dehydrate ikaite; anneal random distribution …
Good agreement with expt structure factor

## Slide 39: Water in hACC
zones of stability for hACC
carbonate-mediated H-bond networks

## Slide 40: Percolating water clusters
Universal scaling behaviour
percolation threshold ~ n = 0.9
underlying hexagonal lattice

## Slide 41: correlated water dynamics
correlated large hops along chains of water

## Slide 42: Classical nucleation
Activated process:
  Favourable “bulk” energy
  Unfavourable interfacial energy
  Critical “cluster” size
Classical Nucleation Theory
Fundamentally Stochastic
Favourable
Unfavourable

## Slide 43: hACC nucleation: classical?
DOLLOP, Raiteri et al.,
Nature Comms, 2011
pre-nucleation clusters Gebauer et al., Science 2008
dense liquid phase Wallace et al., Science, 2014

## Slide 44: Nature of the clusters?
spontaneous clusters dominate?
Random Structure searches
  random arrangement of ions; minimise; repeat
Intelligent Water Drop algorithm
  nature-inspired global optimsation
  erosion of soil to define river valleys
  applications to binary LJ mixtures and Janus particles
    (not yet carbonates)

## Slide 45: Random Structure Searches
random arrangement of ions within sphere
Conjugate Gradient optimisation
~10,000 initial structures for each cluster size (1–40 formula units)
variety of cluster properties
  e.g. energy vs radius of gyration

## Slide 46: Energetics of solvated clusters

## Slide 47: Free energy Landscape
~2 kT
F / eV
nO–Ow

## Slide 48: Long timescale MD: 20–50 mM
“slow” dissolution: convergence from dispersion or initial clusters
dissolution slows with cluster size (concentration)
(requires free energy barrier)

## Slide 49: Long timescale MD: ca. 0.5 M
stable “DOLLOP” behaviour; large clusters

## Slide 50: And higher concentrations: 0.5–1.5 M
0.57 M
stable clusters
DOLLOP
1.1 M
infinite, liquid like (phase transition?)

## Slide 51: Conclusions
Source of new mechanistic insight
  kinetic inhibition; eggshell proteins
  does your predictive model have the right features?
Can capture some elements of intrinsic complexity
  inhibitor polydispersity; nanoparticle structure
  need for intelligent sampling
Progress through data dimensionality reduction
  excellent methods for a handful of dimensions
  need to identify key dimensions
  need to recognise and avoid pitfalls of too few (or wrong) dimensions