## Slide 1: Nanoscale Redox Imaging
Marc Baghdadi
Supervisor: Prof. Pat Unwin

## Slide 2: Outline
What is electrochemistry?
The technique – SECM and IC-SECM
Why nanoscale?
Fabrication of platinum ultramicroelectrodes
Testing Pt tips
  CVs, ACs
Scanning hard surfaces
  Gold bands, Palladium nanowires
Scanning soft surfaces
  Maize roots

## Slide 3: What is electrochemistry?
Study of chemical reactions (redox reactions) taking place in a solution, and involving electrical currents and potentials
Consists of electron transfers between an electrode and electrolyte (solution with ions)

## Slide 4: Typical Electrochemical cell

## Slide 5: Conventional Scanning ElectroChemical Microscopy
Scanning probe microscopy technique
Ultramicroelectrode (UME) tip held at constant height (z-direction) above sample
Sample scanned in x and y directions, with the electrochemical response measured
S. Amemiya, A. J. Bard, F. F. Fan, M. V. Mirkin, P. R. Unwin, Scanning Electrochemical Microscopy, Annu. Rev. Anal. Chem. 2008. 1:95-131

## Slide 6: Typical SECM set-up

## Slide 7: The Problem
Are changes in measured current due to topography or activity changes in the substrate?

## Slide 8: A Solution – IC-SECM
Intermittent Contact SECM integrates UMEs into Atomic Force Microscopy (AFM)
Tip oscillated at constant amplitude through application of a small AC positional perturbation
Amplitude damped as tip approaches surface
Oscillation damping is detected, and is fed back during scanning to keep the tip-surface separation constant

## Slide 9: Why nanoscale?
Essential for subcellular-level studies of biological systems
Nanoelectrodes provide higher signal-noise ratio
Also provide higher mass-transfer rates under steady-state conditions
Leads to much higher spatial resolution
R. W. Murray, Nanoelectrochemistry: Metal Nanoparticles, Nanoelectrodes, and Nanopores, Chem. Rev. 2008, 108, 2688–2720

## Slide 10: Fabrication of Platinum UMEs
B. B. Katemann, W. Schuhmann, Electroanalysis 2002, 14, 22-28

## Slide 11: Well-Pulled Pt Tip
Inner glass wall sealed around wire
Unbroken wire to end of tip

## Slide 12: Badly-Pulled Pt Tips
Broken wire
Wire stops too soon

## Slide 13: Polishing Pt Tip
Polished back by holding tip against 0.1μm micropolisher disc for few seconds.
Alternatively, cut tip using FIB (focused ion beam)
Pt wire

## Slide 14: Testing Pt UMEs

## Slide 15: Cyclic Voltammograms (CVs)
V
t
Limiting current ~ 45pA
⇒ Tip radius of ~ 200nm

## Slide 16: Approach curves
Inert surface
Conductive surface

## Slide 17: Scanning Gold Bands
First line

## Slide 18: Scanning Nanowires
Nanowires
Feedback mode scan
Substrate generation tip collection scan

## Slide 19: Scanning Maize Roots

## Slide 20: Conclusion and Further Work
Nanoelectrodes have successfully been introduced into IC-SECM for hard surfaces
Vary oscillation frequency/amplitude to transfer to soft surfaces
Move to carbon nanoelectrodes

## Slide 21: Acknowledgments
Warwick Electrochemistry and Interfaces Group
  Prof. Pat Unwin, Rob Lazenby, Kim McKelvey, Mike O’Connell
MOAC
EPSRC