## Slide 1: In situ TEM for understanding materials problems
Alex Robertson
Associate Professor of Physics

## Slide 2
University of Warwick
2
Main campus
New £700M STEM building
Kenilworth Castle
Warwick Castle
WMG

## Slide 3
Introduction – rechargeable aqueous batteries
3
Mildly acidic electrolyte (typically ZnSO4 salt in water)
Separator
Zinc metal anode
Metal oxide cathode
Aqueous electrolyte (not organic)
Safe and non-toxic
Environmentally friendly
Metal anode
High capacity and cycling rate
► Good candidate for grid storage

## Slide 4
The metal anode – comparison of Li and Zn
4
Z. Li and A. W. Robertson. Electrolyte engineering strategies for regulation of the Zn metal anode in aqueous Zn-ion batteries Battery Energy. 2: 20220029 (2023).
Zixuan Li

## Slide 5
Operando electrochemical TEM
5
Sample preservation
E.g. Interface dendrites
Transfer
TEM imaging
Contaminate
Damage
Revert
Capture dynamics
Material evolution
Initial state
Final state
State 1
State 2
State 3
Missed!

## Slide 6
Zn dendrite growth
6
Electrolyte additives
Electrostatic shielding mechanism
Well studied in Li systems
Similar or different in Zn?
► LiCl additive as prototype candidate
X. Guo, G. He, I. Parkin et al. Alleviation of Dendrite Formation on Zinc Anodes via Electrolyte Additives. ACS Energy Lett. 6, 395-403 (2021).

## Slide 7
Standard 2 M ZnSO4 electrolyte (no additive)
7
Yuan Y., et al. Diagnosing the Electrostatic Shielding Mechanism for Dendrite Suppression in Aqueous Zinc Batteries. Advanced Materials. 36: 2307708 (2024).
Yi Yuan

## Slide 8
Standard 2 M ZnSO4 electrolyte (no additive)
8
100 mA/cm2
Electrode (Pt)
Θ = 120°
Electrolyte

## Slide 9
2 M ZnSO4 electrolyte with LiCl additive
9
Yuan Y., et al. Diagnosing the Electrostatic Shielding Mechanism for Dendrite Suppression in Aqueous Zinc Batteries. Advanced Materials. 36: 2307708 (2024).

## Slide 10
2 M ZnSO4 electrolyte with LiCl additive
10
100 mA/cm2
θ = 120°

## Slide 11
Mechanism?
11
Electrode (Pt)
Electrode (Pt)
Electrode (Pt)
Nucleation
Primary nuclei growth
Secondary nucleation and growth
Preferred nucleation sites
No additive – Dendritic
Additive – Block shape
Sharp edges
Blunt edges
Restricted adsorption

## Slide 12
Mechanism – Electrostatic shielding of sharp facets
12
(100)
(002)
Metal anode
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Zn
Cl
Cl
Cl
Cl
Cl
Cl
Cl
Li
Li
Li
Li
Li
Li
Li
Li
Cl
Cl
Side view
Y. Yuan, et al. Diagnosing the electrostatic shielding mechanism for dendrite suppression in aqueous zinc batteries Adv. Mat. 36: 2307708 (2024).

## Slide 13
2D materials – MoS2 Memristors
13
Wells, R and Robertson, A. W. Molybdenum Disulfide Memristors for Next Generation Memory and Neuromorphic Computing: Progress and Prospects. Advanced Electronic Materials. 10: 2400121 (2024).
Rob Wells

## Slide 14
2D materials – MoS2 Memristors
14

## Slide 15
2D materials – MoS2 Memristors
15

## Slide 16
2D materials – MoS2 Memristors
16

## Slide 17
Acknowledgements
17
The group
The funders
The EM RTP