## Slide 1: Mapping electric fields of operando devices in the electron microscope

## Slide 2: In-situ TEM biasing
micro-electromechanical systems (MEMS) chip
Metal Contacts on a SixNy membrane
DENS Solutions Lightning Biasing and Heating Holder
Notes: In the EMRTP we have the aberration corrected JEOL ARM, samples are placed inside through the side entry port. Using specialised holders from DENS Solutions we are able to apply an electrical bias and/or heat the sample. All of the electronics need to feed through the metal pole of the holder to the metal pin contacts at the end. The biasing and heating at the sample is done by the SixNy MEMS chip you can see there, patterned metal electrodes on a Silicon nitride membrane.

## Slide 3: FIB Preparation
Lift out cross-section of Semiconductor device
Attach between 2 metal contacts of MEMS chip

## Slide 4: Keeping it simple with a Silicon diode

## Slide 5: Mapping Electric Fields – 4D-STEM
23 mrad
mrad
2 mrad
0.2 mrad
Increasing Signal-to-Noise Ratio + Detection Limit
Increasing Spatial Resolution
Notes: The whole story is a little more complex and the convergence semi-angle plays a massive part.

## Slide 6: Mapping Electric Fields – 4D-STEM
In-Plane Electric Field
Planck’s Constant
Beam Deflection (Centre of Mass)
Electron Wavelength
Electron Relativistic Velocity
Projected Thickness of Field
Electron Charge
Notes: The way 4D-STEM works is that we transmit a converged electron beam through a sample and record the resulting diffraction pattern on a direct electron detector. If the electron beam transmits through an electric field then the beam is tilted in real space, which corresponds to a shift in diffraction space. So if we place the central disc of the diffraction pattern on our detector and look at the weighted average of the intensities in each pixel position we can find the centre of the diffraction pattern or the centre of mass. So with the equation on the right here we can calculate the in plane electric field from the tilt angle of the beam measured by CoM

## Slide 7: Centre of Mass
CoM X (μrad)

## Slide 8: Mapping Electric Fields - Electron Beam Induced Current (EBIC)
N-Type
Semiconductor
P-Type
Semiconductor
1. Electron beam transmits through sample
e-
e-
e-
e-
e-
e-
e-
2. Electron-hole pairs are generated in the sample
3. Electron-hole pairs are separated in the presence of an electric field
4. Collect the generated current
A
Notes: And by closing the circuit at both ends we can collect the generated signal, so one end we connect to our collection apparatus (amplifier + ammeter) and the other end to ground.

## Slide 9: Biasing a Silicon Diode
Reverse Bias -2 V
Forward Bias +2 V
0 V
p-n junction
p+/psubstrate interface

## Slide 10: Biasing a Silicon Diode

## Slide 11: EBIC Measuring Diffusion Length

## Slide 12: 4H-SiC Metal-Oxide-Semiconductor Capacitor (MOSCAP)

## Slide 14: Thank You
Supervisors:
Ana M. Sanchez
Richard Beanland
PhD Student:
Yining Xie
Special Thanks to the University of Warwick Electron Microscopy Research Technology Platform (EM-RTP)
Merlin Direct Detector, Point Electronic EBIC System, and Dr. Moynihan’s Postdoctoral Research are all funded by EPSRC grant EP/V028596/1
Si diode sample provided by
David Cooper CEA LETI
4H-SiC MOSCAP sample provided by
Peter Gammon & Arne (Ben) Renz

## Slide 15: Mapping the Electric Field – 4D-STEM

## Slide 17: Biased 4D-STEM & EBIC in Reverse Bias