## Slide 1: Accessing conventional synthetic polymers at the atomic level
Dr Evelina Liarou
Department of Chemistry
University of Warwick

## Slide 2
Dr Evelina Liarou
Department of Chemistry
University of Warwick
Polymer Chemists and Atomic Resolution
Accessing conventional synthetic polymers at the atomic level

## Slide 3
Synthetic Macromolecular Chemistry – Overview
The Mechanism

## Slide 4
Synthetic Macromolecular Chemistry – Overview
The Synthesis
The Mechanism

## Slide 5
Synthetic Macromolecular Chemistry – Overview
The Synthesis
The Application
The Mechanism

## Slide 6
Synthetic Macromolecular Chemistry – Overview
The Synthesis
The Application
The Mechanism

## Slide 7
Synthetic Macromolecular Chemistry – Analysis
SEC
NMR
+
-
-
-
-
MALDI
Average molecular weight
&
Average Ð
Low molecular weights
&
Average functionalization
Qualitative functionality
Low molecular weights
&
Linear polymers
Established polymer characterization

## Slide 8
The resolution gap
Precise Synthesis/Sequence Defined Polymers
Atomic Level Polymer Imaging (?)

## Slide 9
Common synthetic polymers: towards the atomic level
Step 1: Overcoming the polymer composition

## Slide 10
Common synthetic polymers: towards the atomic level
Step 1: Overcoming the polymer composition– make it visible
Wilson et al., J. Am. Chem. Soc. 2015 137 (12), 4215-4222

## Slide 11
Common synthetic polymers: towards the atomic level
Step 2: ADF-STEM – image it
8 MX magnification – 0.5 mg/mL

## Slide 12
Common synthetic polymers: towards the atomic level
Step 2: ADF-STEM – image it
8 MX magnification – 0.5 mg/mL
Step 3: Optimization
8 MX magnification – 10 μg·mL-1

## Slide 13
Common synthetic polymers: towards the atomic level
Step 2: ADF-STEM – image it
8 MX magnification – 0.5 mg/mL
Step 3: Optimization
8 MX magnification – 10 μg·mL-1
Step 4: SPC imaging

## Slide 14
Common synthetic polymers: towards the atomic level
Polymer | Mn,SEC | DPn,SEC | Mw,SEC | Ð | MW,DOSY | DPn,DOSY | Mn,STEM | DPn,STEM | ÐSTEM
PAsAm10 | 5,700 | 21 | 6,300 | 1.10 | 2,500 | 9 | 2,300 | 8 | 1.30
PAsAm20 | 7,900 | 29 | 8,700 | 1.10 | 6,900 | 25 | 7,500 | 28 | 1.20
PAsAm50 | 12,100 | 45 | 13,900 | 1.15 | 9,600 | 35 | 11,000 | 40 | 1.10
PAsAmFRP | 218,000 | 804 | 509,000 | 2.30 | 101,700 | 375 | 113,000 | 417 | 1.60
Liarou. E.*, et al., J. Am. Chem. Soc. 2024 146 (50), 34292-34297

## Slide 15
Common synthetic polymers: towards the atomic level
Liarou. E.*, et al., J. Am. Chem. Soc. 2024 146 (50), 34292-34297
Other elements
Commodity polymers

## Slide 16
Common synthetic polymers: towards the atomic level
Commodity Polymers
*Manuscript in preparation
Macromolecular Architectures
UHMW Polymers[1]
Organometallic Polymers
M-Oxo Polymers
[1]Ratajczyk, M.; Liarou, E.* et al., Macromol. Chem. Phys. 2026, 227 (3), e00492.

## Slide 17
Nat Commun., 11, 1486 (2020) , Chem. Sci., 2020, 11, 5257-5266, J. Am. Chem. Soc., 2022, 144, 15, 6954–6963, J. Am. Chem. Soc. 2024 146 (50), 34292-34297

## Slide 18
Acknowledgments
Dr. Arkadios Marathianos (RTP)
Maciej Ratajczyk (MRes)
Prof. Ana Sanchez
Dr. Yisong Han (RTP)
Prof. David Haddleton
Prof. Paul Wilson
Jared Taylor (MChem)
Amirah Mohammed (MChem)
Dr. Alex Magiakos (PDRA)
Dr. Seb Pike
Prof. Athina Anastasaki (ETH-Zurich)
Prof. Christopher Barner-Kowollik (KIT)
Prof. Joe Patterson (UC Irvine)
Prof. Filip Du Prez (Ghent University)
Prof. Kelly Velonia (UCrete)
Prof. Hermis Iatrou (UAthens)
Prof. Paola Manini (UNaples)
Prof. Dmitri Golberg (QUT)
Funding
Team & University of Warwick
International Collaborations