## Slide 1
Structure – Property Studies of Nanoscale Materials Using Precession Electron Diffraction in TEM
Brussels, Belgium
nanomegas.com
Thanos Galanis Application Specialist
EM RTP Facility Open Day, Warwick, April 22nd 2026

## Slide 2
Imaging REAL space
www.nanomegas.com
Introduction
High Resolution TEM image
Mg Crystal
Nanoparticles

## Slide 3
Imaging RECIPROCAL Space
www.nanomegas.com
Introduction
Electron Diffraction
Ta O5
Every spot corresponds to crystal planes
&
are indexed by Miller indices: h k l

## Slide 4
Image formation in TEM
Back Focal
Plane
Image
Plane
Objective
Lens
Sample
e-
Point resolution
Information limit
Electron diffraction
High resolution image
REAL and RECIPROCAL Space in TEM
www.nanomegas.com
Introduction
Transmission Electron Microscopy

## Slide 5
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Hardware & Software
based applications
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
e Pair Distribution Function mapping

## Slide 6
De-scan
Scan
Sample
Conventional Diffraction Pattern
Precession…
Precession Diffraction Pattern
Precession Electron Diffraction
www.nanomegas.com
Courtesy: C. Own & L. Marks
Increasing Precession angle:
Higher resolution
higher order reflections
Reduce of dynamical effect
Close to kinematical / real reflections
Less sensitivity to specimen thickness / bending
Introduction

## Slide 7
Precession Electron Diffraction
www.nanomegas.com
Increasing Precession angle:
Higher resolution
higher order reflections
Reduce of dynamical effect
Close to kinematical / real reflections
Less sensitivity to specimen thickness / bending
Introduction

## Slide 8
PED Applications available for every TEM
Introduction
FEG |LaB6 sources
100-300kV
www.nanomegas.com

## Slide 9
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Hardware & Software
based applications
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
e Pair Distribution Function mapping
Precession enhanced 4D-STEM
4D-SPED

## Slide 10
Pseudo-Parallel
beam
Electron Diffraction pattern
4D-SPED Data Acquisition
Scanning Precession Electron Diffraction
www.nanomegas.com
4D-SPED: Scanning Precession Electro Diffraction Applications
No precession
Introduction
Precession Enhanced 4D-STEM

## Slide 11
Scanning
Precession Enhanced
Electron Diffraction pattern
4D-SPED Data Acquisition
Scanning Precession Electron Diffraction
Pseudo-Parallel
Precessed beam
www.nanomegas.com
Precession: 0.6o
4D-SPED: Scanning Precession Electro Diffraction Applications
Introduction
Precession Enhanced 4D-STEM

## Slide 12
Scanning
Pseudo-Parallel
Precessed beam
4D-SPED Data Acquisition
Scanning Precession Electron Diffraction
www.nanomegas.com
4D-SPED: Scanning Precession Electro Diffraction Applications
Introduction
Precession Enhanced 4D-STEM

## Slide 13
4D-SPED Data Acquisition
Scanning Precession Electron Diffraction
www.nanomegas.com
4D-SPED: Scanning Precession Electro Diffraction Applications
Introduction
Scanning
Pseudo-Parallel
Precessed beam
Precession Enhanced 4D-STEM

## Slide 14
Pseudo-Parallel
Precessed beam
Scanning
Completed
4D-SPED Data Acquisition
Scanning Precession Electron Diffraction
www.nanomegas.com
4D-SPED: Scanning Precession Electro Diffraction Applications
Introduction
Precession Enhanced 4D-STEM

## Slide 15
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
e Pair Distribution Function mapping
Study of the properties in nm-scale of:
alloys, metals, nanoparticles, semiconductors, minerals, nanowires, ceramics, films, batteries, etc..

## Slide 16
www.nanomegas.com
Orientation Map
Grain Boundaries Map
Virtual Dark Field Image
Grain Size Distribution
Texture Analysis
Correlation Coefficient Map
Introduction
Orientation & Phase Map
ASTAR: Orientation & Phase Mapping
First turnkey application using 4D-STEM data acquisition since 2007,
few years before the 4D-STEM terminology was introduced

## Slide 17
www.nanomegas.com
ASTAR: Orientation & Phase mapping in nm scale
Spatial Resolution of 1nm
In Situ Heating / Pd Material
Orientation Map
3D Detailed Projection
Texture Analysis
Phase Map
Interactive Virtual Dark Field
Fe
Fe14Nd2B
Fe2B
NdH2
Introduction
Orientation & Phase Map

## Slide 18
ASTAR: Copper and Copper lines
Courtesy of Profs. K. Barmak, Columbia Univ. NY & A.D. Rollett CMU Pittsburgh PA
Nano-twinned copper
Orientation map for a 111-nm-thick Cu film imaged in plan view combined to the correlation index map (grayscale).
(TECNAI F20 - Courtesy of Profs. K. Barmak Columbia Univ. NY and A.D. Rollett CMU Pittsburgh PA)
Physical Metallurgy Chap. 10, 2015 (David Laughlin ed.)
Copper lines (cross-sections and longitudinal section) in microelectronic devices
Grain size statistics INCLUDING twin boundaries
Grain size statistics WITHOUT twin boundaries
Index map
Orientation map
Grain boundaries
Twin boundaries
Bright-field image
Unpublished work
EXAMPLES

## Slide 19
ASTAR: Microelectronic devices
EXAMPLES
Tungsten
Copper
TiN
Si2N4 (amorphous)
SiO2 (amorphous)
Amorphous
Orientation and phase maps
Phase map
Diffraction pattern of an amorphous phase

## Slide 20
e Pair Distribution Function mapping
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
Study of strain / deformation in nm-scale of:
semiconductors, metals, ceramics, etc..

## Slide 21
Orientation & Phase Map
Introduction
Strain Mapping
www.nanomegas.com
topspin
Strain Mapping
Single crystal grain area calculated
εxx
εyy
0
100
200
300
0.010
0.000
0.005
Position (nm)
Strain
εxx
0.010
0.005
0.015
Strain
0
100
200
300
Position (nm)
εyy
Strain Profile
pMOS device
PED Strain Mapping
Spatial resolution: 1-5 nm
Strain Sensitivity: >0.02%
TopSPIN: Strain mapping in nm scale and high sensitivity

## Slide 22
Orientation & Phase Map
Introduction
Strain Mapping
topspin
TopSPIN: Strain mapping in nm scale and high sensitivity
TopSPIN strain | Precession 1o
TopSPIN strain | No Precession
200KV NonProbe Corrected, ScanStep 1nm, spot8, C2ap20um, 144pixels/frame, 12 bit depth, 20mspf
εxx
εxx
εxx
εxx
εyy
εyy
εyy
εyy
Precession ON
Precession OFF
Courtesy of Dr. Joaquim Portillo
Si / SiGe

## Slide 23
e Pair Distribution Function mapping
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
Electric Field studies in nm scale
Different phases Interface, quantum wells, p-n junctions, batteries,

## Slide 24
Precession Electron Diffraction Solutions – Electric field Studies
Electric Field
Data acquitition using NanoMEGAS scan engine and precession generator
Distortion-corrected diffraction patterns
Compatible with 8- to 16-bit data, pixel sizes ranging from 128×128 to 1024 ×1024 or more
Automated user-friendly workflow.
Precession is essential for samples >50nm of thickness
Data processing
  Reference selection from any position of the acquired area
  Automated beam offset correction from scanning
  Adjust rotation of scanning and TEM azimuthal rotation
  Full set of offset maps (proportional to EF)
  Integrated Profiles of COMx, COMy, COMmag
  Calculation and diagrams of Αpparent EF and Αpparent potential.
  Reference color map with display option.
www.nanomegas.com

## Slide 25
Electric field Studies – STOCa dopped semiconductor
SrTiO3
Sr0.99Ca0.03TiO3
AlO amorphous
Au
LaAlO3
20nm
7nm
Universitat Rovira i Virgili, Tarragona
Collaborations: Sergi Plana Ruiz, sergi.plana@urv.cat
Jaume Gazquez, jgazquez@icmab.es
R. Guzman, rguzman@icmab.es
NanoMEGAS: Joaquim Portillo,
Thanos Galanis
Potential difference is expected to be detected at the 1% mol of Ca-dopped STO phase: Sr1-xCaxTiO3.
Heterostructures: Visualization of the charge distribution in LAO // AlOx // Sr0.97Ca0.03TiO3
Electric Field

## Slide 26
Electric field Studies – STOCa dopped semiconductor
SrTiO3
Sr0.99Ca0.03TiO3
AlO amorphous
Au
LaAlO3
20nm
7nm
Universitat Rovira i Virgili, Tarragona
JEOL 2100
Scan and Precession Generator: DigiSTAR P2010
Acquistion platform: TopSPIN acq
Camera: Gatan OneView
Step size: 1nm
Exp time 10ms
Convergence semi angle: ~3mrad
Precession angle: 0.8o
Precession frequency: 1000Hz
Potential difference is expected to be detected at the 1% mol of Ca-dopped STO phase: Sr1-xCaxTiO3.
Heterostructures: Visualization of the charge distribution in LAO // AlOx // Sr0.97Ca0.03TiO3
Electric Field

## Slide 27
Electric field Studies – STOCa dopped semiconductor
Heterostructures: Visualization of the charge distribution in LAO // AlOx // Sr0.97Ca0.03TiO3
No PED
PED
10 nm
Why Precession?
Limited contrast inside the transmitted beam, due to dynamical effect reduction:
Uniform intensity into the transmitted beam.
Improved COM calculations.
More reliable and reproducible results.
CoM map
Electric Field

## Slide 28
Electric field Studies – STOCa dopped semiconductor
STOCa: 3% Ca dopped STO
eEF | No Precession Rotation correction
Representative DP without Precession
eEF | Precession 0.8o Rotation correction
Representative DP with Precession
SrTiO3
Sr0.99Ca0.03TiO3
AlO amorphous
Au
LaAlO3
20nm
7nm
VBF
COMx
COMy
EF
Electric Field

## Slide 29
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
e Pair Distribution Function mapping
      Semi-Crystalline and Amorphous Materials analysis
      spot OR scanning
      Semiconductors, Polymers, Batteries, Solar Cells, Sensors Catalysts, Glasses, Thin Films, etc

## Slide 30
Diffraction Patterns: Crystalline vs Nanocrystalline/Amorphous
🔵 Crystalline Materials:
  Sharp Bragg peaks (intense, well-defined)
  Easy to solve structure with conventional crystallography
🔴 Nanocrystalline & Amorphous Materials:
  Broad, diffuse diffraction rings
  Standard crystallography fails → need alternative methods Examples: Glasses, liquids, polymers, oxides…
🔷 Alternative Method to analyze Nanocrystalline & Amorphous Materials > PDF :
  Applicable to both crystalline and amorphous materials
  Extracts local atomic structure and short-range order information from diffuse scattering
  Complements traditional crystallography, especially when Bragg peaks are weak or absent
PDF
www.nanomegas.com

## Slide 31
A total pair-distribution function (PDF) is obtained by repeating this process systematically by placing each atom in the origin.
Pair Distribution Function G(r) is probability of finding an atom in a distance r
www.nanomegas.com
PDF: Pair Distribution Function– Characterization of Amorphous materials
X
2 Å
1
2
3
4
5
6
r (Å)
R (Å -1)
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF

## Slide 32
Interatomic
distances
Workflow: From Diffraction Patterns to PDF
PDF
2D Diffraction Pattern
Raw experimental data
1D Intensity Profile
Azimuthal integration
Reduced Structure Function F(Q)
Normalization & transformation
Pair Distribution Function G(r)
Atomic distances revealed
Q: f(Q): Atomic scattering factor (form factor), ⟨ f²(Q) ⟩_composition: Mean square scattering factor ⟨ f²(Q) ⟩ = Σ cᵢ fᵢ²(Q) ,⟨ f(Q) ⟩_composition: Average scattering factor over the sample composition ⟨ f(Q) ⟩ = Σ cᵢ fᵢ(Q)
Revealing interatomic distances across crystalline, nanocrystalline, and amorphous materials
I(Q) → S(Q) → F(Q) → G(r)
PDF
www.nanomegas.com

## Slide 33
Layer 2 : first-neighbor Si–N 1.68 Å, consistent with silicon nitride (SiₓNᵧ)
Crystalline Part
Layer 1 : first peak at 1.60 Å — matches Si–O; no carbon; likely SiO𝑥
PHASE IDENTIFICATION
ePDF Mapping: Analysis of amorphous Semiconductor material |2- QOI Map
ePDF QOI map: Variation of the peak position
Layer 1
Layer 2
PDF
www.nanomegas.com

## Slide 34
e Pair Distribution Function mapping
topspin
Strain Mapping
Orientation & Phase Mapping
3D diffraction tomography
e Pair Distribution Function
Precession Electron Diffraction Solutions
www.nanomegas.com
Electric Field Studies
Introduction
GaAs/AlAs (001) interface
Si3N4
SiO2
Electron Crystallography
Precession enhanced 3DED; MicroED
Determination of crystal structures of minerals, zeolites, MOFs, pharmaceuticals, proteins, etc

## Slide 35
Why to Use Electron Crystallography?
www.nanomegas.com
Small crystals
<0.5 micron in size, progressively broader
X-Ray reflections peaks
Overlapping Powder X-Ray peaks
poorly crystallized materials
X-Ray Crystallography Methods - Limits
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF
PED tomography

## Slide 36
www.nanomegas.com
Cell parameter and symmetry determination from nm single crystals
Powder pattens: sum of individual nanocrystals
Why to Use Electron Crystallography?
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF
PED tomography

## Slide 37
Select crystal & area for
data acquisition
Crystal Image
Precession Electron Diffraction
Record PED pattern by TEM detector
Precession Electron Diffraction
Record PED pattern by TEM detector
Tilt 1 degree
Precession Electron Diffraction
Record PED pattern by TEM detector
Tilt 1 degree
Tilt 1 degree
Precession Electron Diffraction
Record PED pattern by TEM detector
Track Crystal under the Beam
Tilt every 1 degree
Precession Electron Diffraction
Acquire PED pattern every 1o
Track Crystal under the Beam
Precession Electron Diffraction Tomography (PEDt) – Solve crystal structures
www.nanomegas.com
Collect series of PED patterns every 1o
Tilt range for cell parameters determination: -30o to +30o
Tilt range for structure determination: -60o to +60o
Completeness of reciprocal space
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF
PED tomography

## Slide 38
Precession Electron Diffraction Tomography (PEDt) – Solve crystal structures
www.nanomegas.com
PED patterns every 1o
Reciprocal Space Reconstruction
Solving Crystal Structure
Final Structural Model
Cell parameters determination
ED intensities extraction
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF
PED tomography

## Slide 39
ITQ43_Zeolite
HAPY_Mg2Al(OH)2AlSiO6
PEDt tomography
Paracetamol
MFU4L_MOF
Precession Electron Diffraction Tomography (PEDt) – Solve crystal structures
www.nanomegas.com
minerals
Pharmaceuticals & Proteins
Microporous minerals
catalysts
Pigment Yellow
pigments
batteries
Light-Emitting Diodes
Introduction
Orientation & Phase Map
Strain Mapping
Electric Field
e-PDF
PED tomography

## Slide 40
NanoMEGAS.COM
www.nanomegas.com
Applications details
Literature on PED techniques
Past & Forthcoming Webinars
Brussels, Belgium
nanomegas.com

## Slide 41
Thank you!
Photo from NanoMEGAS annual meeting, Crete, June 2024